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                               Ref:  DOP 1073

DECLARATION OF PERFORMANCE                                                                                               in accordance with Annex 111 of Regulation (EU) No. 305/2011
( Construction Products Regulation )

1. Unique identification code of the product type:

ULTRATILE FIX PROGRIP FX WHITE

2. Type, batch or serial number or other identifying mark to identify the construction product as set out in Article 11 (4):

Product formulation reference X2009
3. Intended use as foreseen by the manufacturer of the construction product in accordance with harmonised technical specification:
Improved deformable cementitious adhesive with reduced slip and extended open time

4. Name, registered trade name or registered trade mark and contact address of the manufacturer as set out in Article 11 (5):

Instarmac Group plc
Birch Coppice Industrial Estate

Danny Morson Way, Dordon

Tamworth B78 1SE

United Kingdom

5. When applicable, the name and contact address of the authorised representative who has received a mandate for the tasks set out in Article 12 ( 2 ):

Not relevant
6. System or systems for assessment and verification of constancy of performance of the construction product in accordance with Annex V:

System 3 + 4
7. In the case of a declaration of performance concerning a construction product that is covered by a harmonised standard:

The notified body Ceram, No. 1289 has carried out initial type testing to System 3 and issued Test report No. (124246) - 17184
8. In the case of the declaration of performance concerning a construction product for which a European Technical Assessment has been issued.

Not relevant

9. Declared performance

Essential characteristics
Performance

Harmonised technical specification
Bond Strength as:

Initial tensile adhesion

2.1 N/mm2




Durability for tensile 

Adhesion:

After heat ageing

1.7 N/mm2




After water immersion

1.4 N/mm2


BSEN 12004:2007+A1:2012
After freeze/thaw cycles
1.4 N/mm2




Reaction to Fire


Class E WFT

Release of dangerous

Substances


See MSDS

CLASSIFICATION - C2 TE S1

10. The performance of the product identified in items 1 and 2 in conformity with the declared  performance set out in item 9. The manufacturer as defined in number 4 is solely responsible for drawing up this declaration of performance.

Signed for on behalf of the manufacturer by:
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Tamworth – 31.08.18
................................................ (Signature)         ............................................ (Place & Date Issued) 

Chris Murphy - Technical Director
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